## Slide 1
BINDT Aerospace workshop – UT TFM for LMDw
Tom Bertenshaw
Principal NDT Research Engineer
Export Control - Technology Uncontrolled data - The documents within this transmission contain NO technical data subject to the "UK Export Control Act 2002 or EU Dual-Use Regulation (Council Regulation (EC) No 428/2009), as amended. Export Classification: NSR

## Slide 2: BINDT Aerospace workshop – UT TFM for LMDw
    Presentation Content
    Overview of Research project
    Previous work
    Gaps / Issues
    Planned tests
    Outcome
    Ongoing work and Future work
Legally privileged and confidential

## Slide 3: BINDT Aerospace workshop – UT TFM for LMDw
    Overview of Research Project:
    No NDT inspection processes has yet been developed for LMDw parts, which meets the inspection criteria.
    My role has been to implement a new inspection process using the “Total Focusing Method” (TFM), initially for TRL accreditation but ultimately to support part qualification.
    The goal was to demonstrate inspection capability for a Ti64 aerospace bracket, manufactured by LMDw to TRL5 maturity
2020 |  |  |  | 2021 |  |  |  | 2022 |  |  |  | 2023 |  |  |  | 2024 |  |  |  | 2025
Lit review
TRL3 passed
Exploratory NDT work begins
TRL4 passed
TRL5
Equipment procurement
Today
NDT activities paused
Prep for TRL5 starts
Timeline
H-Sections
Fatigue walls
Legally privileged and confidential

## Slide 4: LMDw: NDT technique development for TRL4
  Previous work - Test Plan
    Test blocks manufactured from LMDw Ti walls
    Inspection from baseplate
      use standard Pulse Echo Phased Array
      Use FMC/TFM technology (2D encoded)
    direct wall inspection
      use standard Pulse Echo Phased Array
      Longitudinal & Shear wave techniques
      Through Transmission
    Artificial Defects:
      Spherical bottomed holes
      Flat bottomed holes
      EDM notch defects
    Scan time / Setup time
Test Blocks
Stepped blocks PE FMC/TFM inspection from baseplate
Inspection from web
Use PAUT, Shear wave and TT inspection techniques
SBH and EDM notch defects
Export Classification - NSR
Legally privileged and confidential
Notes: Test blocks manufactured from LMDw Ti walls will look at different ways of inspecting these components.
It will also assess different ways of detecting defects at different orientations
Defects can take many forms – some literature has shown it is possible to create cracks parallel to the web surface
Spherical bottomed holes were used in these stepped blocks (as indicated by red boxes)
They are the most difficult to image
Representative of voids

## Slide 5: LMDw: NDT technique development for TRL4
  Previous work - Results
    Defect Detection with TFM using stitched scans
C-scan gated around defect on second step
B-scan
Export Classification - NSR
Legally privileged and confidential
Notes: Notes:
There are small improvements required
Slight misalignment in B-scan is to small change in probe offset (1-2mm)

## Slide 6: LMDw: NDT technique development for TRL4
  Previous work – conclusions from tests
    Principle technique used was longitudinal Pulse Echo FMC/TFM inspection from the bottom of the baseplate
    Test blocks are similar to those described in AMS-STD-2154E
    Use of TFM stitched scans
    Preferred scan orientation / test setup
    Other observations
      Effect of component distortion
      Effect of grain boundary noise
      Scan orientation
      Probe alignment, probe offset and velocity correction – critical parameters for TFM in a scanning tank
      Speed of System for FMC/TFM acquisition
Export Classification - NSR
Legally privileged and confidential

## Slide 7: BINDT Aerospace workshop – UT TFM for LMDw
    Gaps & Issues
    Component distortion and misalignment
    Standard compliance – standards that are meant for wrought components can guide test block definition
    Coverage – For deep/high walls, another means is needed to inspect the walls: Use shear waves from the side
    Detectable defect size: GKN M&P require smaller defects to be found to show we can meet HCF properties
Waterpath can vary due to component alignment and distortion
Region of inspection
Lack of fusion type defects
Defect characterisation
TFM inspection from baseplate
Shear wave inspection from side wall (machined)
Void / pore defect
Legally privileged and confidential

## Slide 8: BINDT Aerospace workshop – UT TFM for LMDw
    Planned tests
    Manufacture of updated longitudinal wave test blocks:
      Flat bottomed holes (ASTM E127 compliance)
      Hole sizes Ø0.8mm, Ø0.6mm, Ø0.4mm & Ø0.3mm
    Design and manufacture of shear wave blocks:
      Manufacture IOW AMS 2154E
      Different blocks recommended for area amplitude calibration and Distance amplitude calibration
    Characterisation of real defects vs FBHs in test blocks
Shear wave block iaw AMS2154E – area amplitude cal
DAC block of similar design for 2 angles
Legally privileged and confidential

## Slide 9: BINDT Aerospace workshop – UT TFM for LMDw
    Outcome - longitudinal wave blocks
    Drilling 0.3mm & 0.4mm holes has been problematic – EDM drilling has not worked.
    Machining using a high speed spindle – acceptable results
Awaiting X-ray CT results
Legally privileged and confidential

## Slide 10: BINDT Aerospace workshop – UT TFM for LMDw
    Validation of UT with X-ray CT data
    We took some start/stop regions from the fatigue walls
    The ends were inspected in the immersion tank and all data captured. Measurements of % amplitude were made
    The defects were isolated marked out using a single crystal probe and cut out of the block into small Ti64 cylinders
Waterpath can vary due to component alignment and distortion
Legally privileged and confidential

## Slide 11: BINDT Aerospace workshop – UT TFM for LMDw
    Validation of UT with X-ray CT data
    The Ti cylinders were inspected using the X-ray CT machine currently available to GKN Trollhattan in the PTC centre
    We were able to distiguish between LOF and porosity defects and the angle of LOF defects
X-ray CT reconstruction of Defect ID1
Legally privileged and confidential

## Slide 12: BINDT Aerospace workshop – UT TFM for LMDw
    Shear wave test block characterisation
    Current test blocks for Flat Bottomed Holes (FBHs) look to use ASTM E127 (see section 8.2.3). This doesn’t cover angle beam inspection of FBHs. It refers AMS 2154E in this case.
    Images right are inspections made from 45 degree block defined in ASTM 2154E (see figure 4). It only Area Amplitude Calibration
    There is work to be done to understand the different sensitivity of the ROI.
    The same flaw in B-scan images right have different amplitude with respect to its position from the index point.
    BS ISO 23865 could give guidance on this calibration
Shear wave inspection – flaw at 55°
Shear wave inspection – flaw at 70°
AMS 2154E angle block with FBHs (60° block shown)
FBHs on this face
Legally privileged and confidential

## Slide 13: BINDT Aerospace workshop – UT TFM for LMDw
    Future work
    Part placement for repeatability - Scanning tank encoder upgrades
    Permanent fixtures for calibration blocks mounted in tank
    Improved fixturing to hold parts under test
    Standards development
Legally privileged and confidential
    Ongoing work
    Complete testing on longitudinal and shear wave setups once test blocks have been created
    Update the inspection procedure with view to demonstrate sizing for 0.3 & 0.4mm defects