## Slide 1: INTRODUCTION TO Immersion Ultrasonics
ANDY WARD MinstNDT
Group Level 3
Basic Principles and Practices

## Slide 2: Subjects
What is “immersion”
Who Uses Immersion
General Principles
Application
Project Examples
01
05
04
03
02

## Slide 3: WHAT IS Immersion?
01

## Slide 4: A Brief Description!
Using the principles of ultrasonic inspection, immersion is just another way to couple the sound leaving the probe and entering the component.
There are several ways to do this, but the more common practices are:
  Complete immersion of the component and the probe in liquid (usually water).
  Or a column of water is sent from the probe to the component surface, usually referred to as squirter systems.
  Due to the nature of the type of defect that is being sought, immersion systems will always have some element of mechanical control from simple 3 axis X, Y, Z systems to more complicated 12 axis robotic systems.

## Slide 5: Typical Samples of Immersion Systems

## Slide 6: Why Do Immersion?
  Immersion is used to find defects/or features in a more controlled environment.
  To find defects and features that could not be detected using the more conventional Contact methods.
  Collect and analyse data using software.
    To allow others to see results.
    Store results for reference.
  Repeatability.

## Slide 7: Who Uses Immersion?
02

## Slide 8: Who Uses Immersion?
  The biggest users of immersion tend to be the forging and wrought material industry.
  However the Composite industry is utilising the inspection more frequently.
  This is generally to inspect product destined for the Aero Space industry. It is usually the Primes like Rolls Royce, GE Engines, Snecma, Pratt and Whitney, Honeywell, MTU etc. that set the criteria for such inspections.

## Slide 9: Who Uses Immersion?
  The Raw material suppliers also use the Immersion method in some form to inspect their product, to ensure it meets the requirements of industry standards such as AMS-2154, 2630, 2631, RRP58002.
  This is most likely to be in the form of Round Billet/Bar or Flat/Square Bar or Plate.

## Slide 10: General Principles
03

## Slide 11: The Big Difference!
  If we compare Contact with immersion one of the big differences is the ‘Water Gap’.
  The ‘Water Gap’ (WG) is the distance from the probe to the surface of the component under inspection. For most applications this is critical and needs to be controlled in such away that this distance remains constant throughout the inspection.
  Why so critical?
  The water gap in most cases has been optimise to allow the probe to perform at its best at a given distance, it could have been adjusted to:
  Optimise the NSR (Near Surface Resolution)
  Focus the inspection at a given depth.
  Give a wide inspection envelope to allow a good NSR and Working Range.

## Slide 12: The Big Difference!
  Velocity of Water 1500m/s
  Velocity of Steel 6000m/s
  For the majority of inspections carried out we do not need to see the initial bang ‘A’ and the water Gap!! So we adjust the delay and range to only see the area of interest.
Probe
FWE
BWE
A
B
C
100mm
100mm
100mm
100mm
A
B
C

## Slide 13: The Big Difference!

## Slide 14: The Big Difference!
Multi Zone
P1
P3
P4
P2
P5
P1 to P5
Z1
Z2
Z3
Z4
Z5

## Slide 15: The Big Difference!
1D Linear Array
1D Annular Array
2D Sectorial annular
2D Matrix
Multi Zone
Using Phased Array

## Slide 16: The Big Difference!
100mm
Distance Amplitude Curve
Distance Amplitude Correction
dB
Distance
Single Probe Inspection With DAC Correction (TCG)

## Slide 17: The Big Difference!
Through Transmission
P1 Send
P2 Receive
Composite

## Slide 18: The Big Difference!
Double Through Transmission
P1
a
b
c
a
b
c
Composite
Reflector (Glass)

## Slide 19: Application
04

## Slide 20: Application.
Ultrasonic Immersion testing as mentioned before is more commonly used for forged components either as raw material or further forged components, like aerospace discs.
However we can take the advantages immersion gives, to look at other components and fabrications.
Such as Composites, welds, brazing, electronics’, castings, complex alloy’s, microstructures etc…
We have the ability to collect data from these types of inspections that can be stored for further analysis and greater scrutiny. There are now systems that allow inspections to be performed remotely by an operator and analysed/sentenced by a inspector (level 2/3) in another country, after inspection or in real time!

## Slide 21: Application.
Advantages:
Repeatability.
  Stable.
  Automation.
  Control.
The ability to detect very small flaws/defects (0.001mm).
Locate flaws/defects more accurately.
Speed!
Data collection.
  Save the data,
  Annalise it after inspection.
  Report and show findings.

## Slide 22: Application.
Dis-advantages:
Setup times can be longer.
Not very portable.
May require Higher level of understanding and skill.
Can have limited scope.
Cost
  Calibration
  Skill
  May require more than one piece of equipment.
  Probes.

## Slide 23: Project Examples
05

## Slide 24: Project Examples.
The following examples are just some of the ways I have used the advantages immersion inspection to inspect components that could not be inspected with other methods.

## Slide 25: Project Examples.
Depth of an EB Weld:
Customer needed to know the depth of penetration that the EB weld was reaching. This had to be between a set acceptance of 2.0mm to 3.5mm. The weld was not fully penetrating and posed several problems in detectability.
There were also misalignment issues where the weld could miss the joint.
1mm

## Slide 26: Project Examples.
Component
Probe
Jig
b
a
c
EB Weld
b
a
c
b
a
Gate
A scan
a
b
c
A scan
Fig 1, No Weld
Fig 2, Welded
Sound Travel
Sound Travel

## Slide 27: Project Examples .

## Slide 28: Project Examples.
Quality of Solder Joints on circuit board:
Customer had issues with the quality of solder joints of busbars to the ceramic plate of the component.
X-ray reviled that there was solder but not how well it is adhered.
1mm
Fig 1

## Slide 29: Project Examples.
Quality of Solder Joints on circuit board:
Again we used the monitor of the back wall principle.
This would show that the better the bond the more transfer of sound through to the next medium and as such would be detectable in the amplitude of the back wall echo.
Busbar
Ceramic

## Slide 30: Project Examples.
Quality of Solder Joints on circuit board:

## Slide 31: Project Examples.
Quality of Solder Joints on circuit board:
Ceramic
Busbar
Solder

## Slide 32
Andy Ward
andy.ward@intertek.com
+44 (0) 1332 257 700
intertek.com