## Slide 1: A Statistical Approach to Ultrasonic Inspection in Complex Geometry
Matt Chandler – m.chandler@bristol.ac.uk
Supervisors:
Prof. Anthony Croxford & Prof. Paul Wilcox

## Slide 2: Overview
Introduction
  Motivation
  Statistical framework
Multivariate statistics
  Wrinkling in CFRP
  Hypothesis testing
Conclusions
1

## Slide 3: Motivation
[1] | Michael Pätzold, CC BY-SA 3.0, via Wikimedia Commons
[2] | Duboyong, CC-BY-SA-4.0, via Wikimedia Commons
Geometrical complexity
Structural complexity
2

## Slide 4: Statistical Framework
25mm
45mm
[3] | Chandler, M. G. et al., NDT & E Int. 142, 103014 (2024)
No SDH
SDH
Probability maps
3

## Slide 5: Wrinkling in CFRP
Interfaces between layers in CFRP act as reflectors of the ultrasonic signal. Regular structure produced in TFM images, which changes when structure is wrinkled.
4

## Slide 6
Autocorrelation
Expect intensity to be highly correlated between layers.
5

## Slide 7
Multivariate Hypothesis Testing
Model , and perform hypothesis testing.
6
Notes: If we model 𝐴_𝐼 from unwrinkled samples as a multivariate normal distribution, we can attempt to perform hypothesis testing as before. Rearrange the results of 𝐴_𝐼 into a vector of length 𝑘, and fit a distribution 𝒩_𝑘. Hypothesis testing then requires the use of the Mahalanobis distance, or the distance of a point from the mean, normalised by the covariance. This accounts for any dependence between the variables – I’ve visualised what that means here for an arbitrary 2-dimensional example. If the null hypothesis is true, 𝑠 will follow the 𝜒^2 distribution, so we can convert to 𝑝-values if needed. I haven’t done that here.

## Slide 8
Multivariate Hypothesis Testing
Model , and perform hypothesis testing.
Compute normalised distance from the mean
6

## Slide 9: -maps vs. Ply Orientation
[4] | Nelson, L. J. et al., Composites A, 104, 108-119 (2018)
 | TFM magnitude
 | TFM phase
 | Single pixel box; (0.11, 0.11)mm,
 | Non-zero area; (0.88, 0.22)mm,
 | Structure tensor method for ply orientation extraction. [4]
 | TFM magnitude
 | TFM phase
 | Structure tensor method for ply orientation extraction. [4]
7
Notes: We can now evaluate how well this method performs at wrinkling detection. In these black-and-white plots, I have computed this distance 𝑠 at each location in the TFM, for two different boxes. The top plot is a 1-by-1 pixel, in which we are considering only the complex-valued image intensity, and in the second, some area is included, finding that we do pretty well with both, however the insight we can make is that by including some area, the noise level in the pristine case is much lower. This is compared to the structure tensor method for ply layer orientation extraction, which finds the angle of each layer, as an alternative approach for wrinkling detection.

## Slide 10: Performance Evaluation
(a) | ROC curves for , single pixel box.
(b) | ROC curves for , , .
(c) | Area under the curve (AUC) for each sample.
(a) | 
(b) | 
(c) | Area under the curve (AUC) for each sample.
8
Notes: We then evaluated the performance of each of these boxes. There’s a lot of information here so I’ll try to walk through it. The first plot shows the ROC curves for the single pixel box 𝑃_1 for each sample, demonstrating a varying performance with severity but in general not bad given that correlation is not really considered. The results from all samples are then aggregated into a single ROC curve drawn with the black line, we can essentially consider this as an average performance. The second plot compares these average results for all four cases considered: the three box sizes and the comparison case. Recall that box 𝑃_2 (orange) uses a similar amount of information to the structure tensor (blue), and yet we find improved performance. The bottom plot breaks this down for each sample, taking the area under the ROC curve as a metric of performance where a value of 1 indicates that the samples are perfectly classified as containing wrinkling or pristine. The key insight is that in general we have improved performance over the structure tensor method for low levels of wrinkling, which G1 shows. The third plot examines the effect of the box size on classification performance, and demonstrates that 𝑃_3 is the optimal box size for this data set, where the colour axis is the area under the aggregate ROC curve, and I’ve marked where each box sits in this space.

## Slide 11: Conclusions
Improvements made to previous work on detection in geometrically- and structurally complex materials.
Evaluation of area shown to improve detection in materials which are highly scattering.
Pristine data must sample all acceptable variation – array position, temperature, material variations, minimum acceptable flaw.
9
Notes: We have found an improved performance compared to a comparison from the literature, however this comes at the cost of abstracting physical meaning. The structure tensor method produces a map of the ply orientation of each layer throughout the image, which has a fairly intuitive meaning. The maps of 𝑠, the distance from the multidimensional normal distribution, do not have an intuitive physical explanation. Indeed, we are sensitive to any deviation from our pristine case, not just in the form of wrinkling.
A caveat associated with this is that we have very nice samples, and significant care was taken to ensure consistency in data acquisition. As a result, we have very tight definition of “pristine”, and any slight amount of wrinkling was considered as a defect. If this were relaxed to have some minimum level of acceptable wrinkling, we expect that this could be included in the distribution ahead of time. However, this would require exhaustive data collection of every acceptable feature ahead of time.

## Slide 12: Future Work
Write thesis.
Alternative samples
  Assume that demonstration on CFRP is applicable to other samples which are also highly scattering, e.g. rubber, titanium, …
Additional prior information
  Low -value (or high -value) null hypothesis incorrect. Not the same thing as a flaw is present.
  Consider alternative hypothesis (i.e. a given flaw is present), likely using multiple matched filter.
10

## Slide 13: Questions?
m.chandler@bristol.ac.uk
/in/mgchandler
/mgchander
✉